FINAL WORK PLAN

Development and Evaluation of an Ag/Porous-Si SERS Substrate for Sepsis Biomarker Detection

1. Objective

Based on the experimental results obtained so far, I propose to investigate a new Ag/Porous-Si SERS substrate as an alternative to the existing Ag/Black-Si substrate.

The objective is not to immediately replace the existing substrate, but to:

- Fabricate porous silicon using a literature-supported electrochemical method.

- Deposit Ag nanoparticles onto the porous-Si structure using a literature-reported Ag deposition method.

- Characterize the resulting substrate.

- Validate SERS activity using R6G.

- Test LPS as the first sepsis biomarker.

- Compare Ag/Porous-Si with the existing Ag/Black-Si substrate under controlled conditions.

- Based on experimental reproducibility, determine the next optimization direction.

- Subsequently investigate NAM and LTA.

The overall approach will be:

Literature replication → Fabrication → Characterization → R6G validation → LPS detection → Substrate comparison → Optimization → NAM/LTA

2. Current Status of the Existing Ag/Black-Si Platform

The experiments performed so far have established the following:

| Test | Current observation |
| --- | --- |
| R6G | Successful and strong SERS response |
| NAM | Not reproducibly detected |
| LTA | Apparent ~1095 cm⁻¹ feature was later identified as a single-pixel artifact |
| Silicon reference | Used to check Raman calibration |
| Substrate activity | Confirmed through R6G response |

Current interpretation

The existing Ag/Black-Si substrate is SERS-active, but reliable detection of the target biomarkers has not yet been demonstrated.

Therefore, the main questions are:

- Is the limitation related to the substrate architecture?

- Is the analyte–Ag interaction insufficient?

- Is the analyte distribution on the substrate affecting detection?

- Is the porous-Si architecture able to provide a more suitable surface for Ag nanoparticle formation and analyte localization?

Based on these questions, I propose investigating Ag/Porous-Si as a second substrate architecture.

3. Proposed Substrate Architecture

The proposed substrate will consist of:

Silicon wafer

↓

Porous Silicon

↓

Ag nanoparticle deposition

↓

Ag/Porous-Si SERS substrate

The conceptual structure is:

Analyte

↓

┌─────────────────┐

│  Ag nanoparticles│

│ •  •  • •  •   │

│  • •  •  • •   │

└─────────────────┘

╔═════════════════╗

║   Porous Si     ║

║  • • • • • •   ║

║ • • • • • • •  ║

╚═════════════════╝

Si wafer

The porous-Si structure will act as a high-surface-area scaffold, while the deposited Ag nanoparticles will provide the plasmonic SERS-active component.

4. Available Silicon Wafer

The available wafer specification is:

- Type: n-type

- Orientation: (100)

- Resistivity: 1–10 Ω·cm

- Surface: Single-side polished

- Grade: Prime grade

- Growth: CZ

Because the available wafer is n-type, the porous-Si fabrication method will be selected based on literature that is compatible with n-type Si rather than directly copying a p-type porous-Si procedure.

5. Available Laboratory Equipment

The available equipment appears suitable for investigating electrochemical porous-Si fabrication.

| Equipment | Proposed role |
| --- | --- |
| ITECH programmable DC power supply | Controlled electrical bias/current |
| CH Instruments electrochemical analyzer | Electrochemical control/measurement |
| Electrochemical cell | Porous-Si fabrication setup |
| Working electrode | Si wafer |
| Counter electrode | Completes electrochemical circuit |
| Reference electrode | Potential control/measurement when required |
| FESEM | Morphological characterization |
| EDS | Elemental confirmation |
| BWTEK i-Raman Plus | Raman/SERS measurements |

The exact instrument configuration and electrochemical cell arrangement will be confirmed before fabrication.

6. Phase I – Literature Verification

Before beginning fabrication, I will identify and verify the most appropriate published porous-Si method for the available n-type Si(100), 1–10 Ω·cm wafer.

The literature review will focus on:

- Si type and orientation

- Resistivity/doping

- Electrochemical configuration

- Electrolyte system

- Current/voltage control

- Etching time

- Illumination requirements

- Porous-layer morphology

- Ag deposition method

- AgNO₃ concentration

- Ag deposition time

- SERS performance

Important principle

I will first select one primary literature protocol that is experimentally compatible with our wafer and equipment.

I will not combine parameters from different papers without justification.

7. Phase II – Porous-Si Fabrication

Objective

Fabricate a reproducible porous-Si layer on the n-type Si wafer.

Planned workflow

n-type Si(100)

↓

Electrochemical cell

↓

Controlled electrochemical anodization

↓

Porous-Si

↓

Rinse/dry according to laboratory SOP

↓

FESEM characterization

The HF-containing electrolyte and operating conditions will follow the selected literature method and the approved institutional HF safety procedure.

Initial goal

The first goal is not maximum SERS enhancement.

The first goal is:

To successfully produce a reproducible porous-Si morphology.

8. Phase III – Porous-Si Characterization

Before Ag deposition, the porous-Si structure will be characterized.

FESEM

To determine:

- pore formation

- pore morphology

- pore distribution

- surface structure

- porous-layer thickness, where measurable

The morphology will be recorded so that it can later be correlated with Ag deposition and SERS performance.

9. Phase IV – Ag Nanoparticle Deposition

After confirming porous-Si formation, Ag will be deposited onto the porous-Si.

The basic process is:

AgNO₃ solution

↓

Ag⁺

↓

Reduction

↓

Ag⁰

↓

Ag nanoparticles

↓

Porous-Si scaffold

↓

Ag/Porous-Si

AgNO₃ will therefore be used as a silver precursor, not as the final deposited material.

Proposed initial approach

Use a literature-reported immersion/electroless Ag deposition method.

The first Ag deposition experiment should reproduce one selected published condition as closely as practical.

After successful deposition, optimization can be introduced systematically.

10. Phase V – Ag/Porous-Si Characterization

The Ag/Porous-Si substrate will be characterized using:

FESEM

To evaluate:

- Ag nanoparticle formation

- particle distribution

- particle morphology

- aggregation

- possible continuous Ag-film formation

EDS

To confirm:

- Ag presence

- Si substrate

Optional characterization

If available:

- UV-Vis spectroscopy

- Additional surface characterization

The objective is to establish a relationship between:

Porous-Si morphology → Ag morphology → SERS performance

11. Phase VI – R6G SERS Validation

R6G will be used as the positive SERS control.

The purpose is to answer:

Does the newly fabricated Ag/Porous-Si substrate provide reproducible SERS enhancement under our 785-nm Raman system?

The R6G experiment will use controlled measurement conditions.

The same measurement conditions should be used for the existing Ag/Black-Si substrate wherever possible.

Comparison

Ag/Black-Si + R6G

versus

Ag/Porous-Si + R6G

Parameters to compare:

- Raman spectrum

- characteristic R6G peaks

- peak intensity

- SNR

- background

- spot-to-spot reproducibility

- substrate-to-substrate reproducibility

12. Phase VII – Reproducibility and Artifact Rejection

The previous LTA experiment demonstrated the importance of distinguishing genuine Raman signals from detector artifacts.

Therefore, future detection criteria will include:

- Expected/chemically plausible Raman feature.

- Reproducibility across multiple measurement spots.

- Reproducibility across repeated measurements.

- Feature extending across multiple detector pixels.

- Difference from substrate/background.

- Concentration-dependent response where applicable.

Important rule

A feature appearing at only one detector pixel will not be considered sufficient evidence for biomarker detection.

13. Phase VIII – LPS Detection

If R6G confirms reproducible SERS activity, the first biomarker to be investigated on Ag/Porous-Si will be:

LPS

The first objective will be:

Demonstrate reproducible LPS detection at a sufficiently high concentration.

The initial experiment will not focus on achieving the lowest possible concentration.

The sequence will be:

High concentration

↓

Detection confirmation

↓

Multiple-spot reproducibility

↓

Repeat measurements

↓

Lower concentration

↓

Concentration-response study

14. Phase IX – Ag/Black-Si vs Ag/Porous-Si Comparison

A controlled comparison will be performed between the two substrate architectures.

Existing substrate

Ag/Black-Si

Proposed substrate

Ag/Porous-Si

For LPS testing, the following should be kept as consistent as possible:

- LPS concentration

- solvent

- deposition procedure

- sample volume

- laser wavelength

- laser power

- integration time

- accumulations

- objective

- spectral acquisition range

- data-processing procedure

Parameters for comparison

| Parameter | Ag/Black-Si | Ag/Porous-Si |
| --- | --- | --- |
| LPS Raman features |  |  |
| Peak intensity |  |  |
| SNR |  |  |
| Background |  |  |
| Spot-to-spot variation |  |  |
| Reproducibility |  |  |
| Substrate morphology |  |  |

The experimental data will determine which architecture should receive further optimization.

15. Phase X – LPS Concentration Study

Only after genuine and reproducible LPS detection is established, a concentration-response study will be performed.

The progression will be:

High concentration

↓

Intermediate concentration

↓

Lower concentration

↓

Lowest reproducibly detected concentration

The following parameters will then be evaluated:

- concentration-response relationship

- reproducibility

- analytical sensitivity

- potential linear range

- LOD, where statistically justified

Principle

LOD and linear range will not be claimed from a single spectrum or isolated Raman feature.

16. Phase XI – NAM Investigation

After establishing the performance of the Ag/Porous-Si platform with LPS, the next biomarker will be:

NAM

The first step will be to test whether NAM can be detected directly on Ag/Porous-Si.

If direct detection remains weak, the next question will be whether the limitation is related to:

- analyte–Ag interaction

- adsorption

- surface localization

- concentration

- Raman cross-section

- need for a selective capture/functionalization strategy

Only then will a suitable surface-functionalization approach be investigated.

17. Phase XII – LTA Investigation

After the LPS and NAM studies:

Ag/Porous-Si + LTA

will be investigated again.

The same rigorous detection criteria will be applied.

The previous ~1095 cm⁻¹ single-pixel feature will remain classified as an artifact rather than a confirmed LTA signal.

18. Phase XIII – Surface Localization

If droplet spreading and coffee-ring effects continue to affect measurements, a subsequent development stage will investigate a localized Ag/porous-Si sensing region.

The objective will be:

To control where the analyte droplet is concentrated relative to the SERS-active region.

This stage will be considered only after the basic Ag/Porous-Si substrate has been experimentally validated.

19. Phase XIV – Optimization

After identifying a reproducible working substrate, systematic optimization will be performed.

Porous-Si parameters

- Porous-Si morphology

- Porosity

- Pore size

- Porous-layer thickness

- Fabrication parameters

Ag parameters

- Ag precursor concentration

- Deposition time

- Ag loading

- Nanoparticle size

- Particle distribution

- Interparticle spacing

Raman parameters

- Laser power

- Integration time

- Number of accumulations

- Objective

- Measurement location

The optimization will be performed one variable at a time or using a defined experimental design rather than random trial-and-error.

20. Overall Experimental Decision Tree

n-type Si(100)

│

↓

Porous-Si fabrication

│

↓

FESEM

│

↓

Porous Si confirmed?

/          \

NO            YES

│              │

troubleshoot         ↓

Ag deposition

│

↓

FESEM + EDS

│

↓

R6G validation

│

SERS reproducible?

/            \

NO              YES

│                │

optimize/modify         ↓

LPS detection

│

reproducible?

/          \

NO            YES

│              │

investigate         ↓

substrate/      concentration

analyte issue       study

│

↓

Compare with Ag/Black-Si

│

↓

NAM + LTA

│

↓

Surface localization/

functionalization

│

↓

Final optimization

│

↓

Sepsis biomarker SERS

platform

21. Immediate Action Plan

The immediate work should be limited to the following sequence:

Step 1

Verify the literature protocol

Select an appropriate published method for the available n-type Si wafer.

Step 2

Confirm equipment configuration

Confirm the electrochemical cell, electrical connections, current/voltage control and any illumination requirement.

Step 3

Fabricate porous Si

Produce the first porous-Si samples following the approved procedure.

Step 4

FESEM characterization

Confirm that porous Si has actually formed.

Step 5

Ag deposition

Reproduce the selected literature Ag immersion/deposition condition.

Step 6

FESEM + EDS

Confirm Ag nanoparticle formation.

Step 7

R6G validation

Confirm SERS activity at 785 nm.

Step 8

LPS

Test LPS at a sufficiently high concentration first.

Step 9

Controlled comparison

Compare Ag/Porous-Si with the existing Ag/Black-Si.

Step 10

Decide the next optimization

Use experimental reproducibility and biomarker response to determine the next stage.

22. Expected Outcome

The immediate objective is not to claim a final sepsis sensor.

The immediate objective is to establish whether:

Ag/Porous-Si can provide a reproducible and experimentally useful SERS platform for sepsis biomarker detection under our laboratory conditions.

If successful, the platform can then be systematically optimized for:

LPS → NAM → LTA → selective capture → multiplex detection → final sensor architecture

23. Key Discussion Points With Prof. Ajay

I would like to obtain confirmation on the following points before beginning the new substrate experiments:

- Porous-Si fabrication: Which literature method should be followed for our n-type Si(100), 1–10 Ω·cm wafer?

- Electrochemical setup: Which available instrument and electrode configuration should be used?

- Ag deposition: Which published AgNO₃ immersion/electroless deposition method should be reproduced?

- Sample number: Should we initially fabricate multiple porous-Si/Ag conditions?

- Characterization: FESEM and EDS before Raman testing?

- R6G: Which existing R6G condition should be used as the standard positive control?

- LPS: Should LPS remain the first biomarker after R6G validation?

- Comparison: Should Ag/Porous-Si and Ag/Black-Si be tested under identical Raman conditions?

- NAM: If direct NAM detection remains unsuccessful, should we investigate surface functionalization?

- Final architecture: Should localized sensing areas be considered after the basic substrate is validated?

Final Proposed Direction

Current status:

Ag/Black-Si → R6G successful → NAM not reproducibly detected → LTA artifact

Proposed next direction:

n-Si → Porous-Si → Ag deposition → Ag/Porous-Si → FESEM/EDS → R6G → LPS → controlled comparison → NAM/LTA → optimization

The purpose of this approach is to move from trial-and-error substrate modification toward a literature-guided, experimentally controlled substrate-development strategy.

Proposed immediate milestone

Fabricate and characterize a reproducible Ag/Porous-Si substrate and establish whether it can produce reproducible R6G SERS response and LPS detection using our existing Raman system.

Final Experimental Plan

Ag/Porous-Silicon SERS Substrate for LPS Detection

1. Overall Objective

The objective is to develop and experimentally validate a silver nanoparticle-decorated porous silicon (Ag/porous-Si) SERS substrate for label-free detection of bacterial LPS.

The experiment will be designed as a step-by-step validation process, rather than directly assuming that the final substrate will work.

The development sequence is:

n-type Si wafer → porous Si → Ag deposition → substrate characterization → R6G SERS validation → LPS detection → concentration study → reproducibility → optimization

The key research question is:

Can Ag nanoparticles deposited on porous silicon provide a reproducible SERS response for LPS under our available 785-nm Raman system?

2. Why We Are Changing the Substrate

Our current Ag/Black-Si substrate is SERS-active, because R6G produces strong Raman enhancement.

However:

- NAM was not reproducibly detected.

- LTA was not reproducibly detected.

- The apparent LTA signal was identified as a detector-pixel artifact.

- The substrate activity itself is therefore not the primary issue.

- The target biomarkers do not necessarily interact strongly with the Ag surface.

- Droplet spreading/coffee-ring effects may reduce the effective analyte concentration in the Raman measurement region.

- The current substrate architecture has therefore reached a point where repeating the same optimization may not provide enough new information.

Instead of simply changing laser power, concentration, or acquisition settings repeatedly, we will investigate a different substrate architecture.

3. Proposed Substrate Architecture

Ag/Porous-Si

The proposed structure is:

Silicon wafer

↓

Porous silicon nanostructure

↓

Silver nanoparticles

↓

LPS

↓

785-nm Raman excitation

↓

Enhanced Raman signal

Function of each component

Silicon

Provides the physical substrate.

Our available wafer is:

- n-type Si

- (100)

- 1–10 Ω·cm

- single-side polished

- prime grade

- CZ silicon

Porous silicon

Provides a nanostructured, high-surface-area scaffold.

The porous structure is expected to provide:

- increased surface area

- nanoscale morphology

- locations for Ag nanoparticle attachment

- altered optical properties

- potential interaction/concentration effects for the analyte

Silver nanoparticles

Silver provides the plasmonic SERS-active component.

The objective is to obtain a controlled distribution of Ag nanoparticles with suitable nanoscale gaps/hotspots.

LPS

LPS is the target sepsis biomarker.

The initial experiment will focus on label-free LPS detection.

4. Important Literature-Based Position

The literature establishes three separate points:

Established

LPS can be detected using Ag-based SERS.

Published LPS SERS work has reported characteristic bands approximately around:

- ~1131 cm⁻¹

- ~1316 cm⁻¹

- ~1366 cm⁻¹

- ~1579 cm⁻¹

- ~1655 cm⁻¹

These values will be treated as reference bands, not as guaranteed peaks in our experiment.

Established

Ag/porous-Si can function as a SERS substrate.

Several studies have demonstrated SERS from Ag-decorated porous silicon using model analytes such as R6G.

Not yet established for our project

There is not enough evidence to claim beforehand that:

Ag/porous-Si + LPS + 785 nm will definitely work.

Therefore, our experiment is specifically designed to test this hypothesis.

5. Experimental Development Strategy

We will divide the experiment into stages.

Stage 1 – Fabricate Porous Silicon

Start with the available:

n-type Si(100), 1–10 Ω·cm wafer.

Porous silicon will be fabricated using an electrochemical/anodization approach appropriate for n-type silicon.

The exact HF concentration, current density, etching time and illumination conditions will be selected from the literature and confirmed with the laboratory's approved HF SOP and Prof. Ajay's guidance.

Important

We will not blindly copy a p-type Si recipe onto the n-type wafer.

The first objective is to establish a reproducible porous-Si morphology.

6. Stage 2 – Create Multiple Porous-Si Conditions

Instead of producing only one substrate, prepare a small controlled matrix.

For example:

| Condition | Etching condition | Purpose |
| --- | --- | --- |
| PSi-1 | Condition A | Lower porosity |
| PSi-2 | Condition B | Medium porosity |
| PSi-3 | Condition C | Higher porosity |

The exact numerical conditions will be finalized from literature and laboratory feasibility.

The variables we may investigate are:

- etching current density

- etching time

- HF concentration

- electrolyte composition

- illumination, if required for n-type Si

Do not change all variables simultaneously.

7. Stage 3 – Characterize Porous Silicon

Before depositing Ag, characterize the porous-Si substrates.

Required characterization

FESEM

Determine:

- surface morphology

- pore structure

- pore size

- uniformity

- surface roughness qualitatively

EDS, where useful:

- confirm Si substrate composition

- later confirm Ag after deposition

The objective is to select porous-Si conditions that produce a reproducible nanostructured surface.

8. Stage 4 – Deposit Silver Nanoparticles

After preparing porous silicon, deposit Ag nanoparticles using a simple Ag⁺ immersion/electroless deposition route as the first approach.

Conceptually:

AgNO₃ solution

↓

Porous-Si substrate

↓

Ag⁺ reduction/deposition

↓

Ag nanoparticles on porous Si

↓

Ag/porous-Si SERS substrate

This route is preferred initially because it is simpler and more reproducible to investigate than introducing complicated lithography, antibodies, aptamers, or multi-metal structures at the beginning.

The Ag deposition conditions will be selected from published Ag/porous-Si studies and adapted only where necessary for our substrate/equipment.

9. Stage 5 – Characterize Ag/Porous-Si

After Ag deposition:

FESEM

Check:

- Ag nanoparticle distribution

- particle size

- aggregation

- coverage

- morphology

- possible nanoscale gaps

EDS

Confirm the presence of:

- Si

- Ag

If available, optical characterization can also be performed to understand the plasmonic response.

10. Stage 6 – R6G SERS Validation

Before using LPS, every candidate substrate must pass the R6G validation test.

This is critical.

We already know from our previous experiments that R6G is a strong SERS reporter.

Therefore:

Ag/porous-Si

↓

R6G

↓

785-nm Raman

↓

Check whether reproducible SERS enhancement occurs.

Purpose

R6G answers:

Is this Ag/porous-Si substrate SERS-active under our Raman system?

It does not answer:

Can this substrate detect LPS?

That distinction must be maintained throughout the project.

11. R6G Validation Criteria

A substrate should not be selected simply because one spectrum looks strong.

A valid substrate should demonstrate:

- recognizable R6G Raman bands

- reasonable signal-to-noise ratio

- reproducibility between different spots

- reproducibility between replicate substrates

- absence of major unexplained artifacts

- consistent spectral shape

If one substrate gives a strong spectrum at only one location, it will not automatically be considered successful.

12. Stage 7 – LPS Experiment

Only after R6G validation will LPS be introduced.

Initial design

Use a controlled LPS concentration series.

A practical first screening range can be centered around the concentrations demonstrated in published LPS-SERS work, rather than immediately attempting extremely low concentrations.

For example:

1 nM → 10 nM → 100 nM → 1 µM → 10 µM

The exact range will be finalized after reviewing the selected primary papers and considering the LPS stock concentration available in the laboratory.

13. LPS Controls

The most important part of the experiment is the control design.

Control 1

Bare silicon / porous silicon + no LPS

Purpose:

Determine the substrate background.

Control 2

Ag/porous-Si without LPS

Purpose:

Determine:

- Ag background

- porous-Si background

- substrate Raman features

- possible Ag-related artifacts

This is the critical blank.

Control 3

Ag/porous-Si + LPS

This is the experimental sample.

Look for features that:

- are absent or substantially different in the blank

- are reproducible

- occur at multiple detector pixels

- occur across multiple measurement spots

- show concentration dependence

Control 4

Ag/porous-Si + R6G

Purpose:

Confirm that the substrate is SERS-active.

14. Raman Measurement

Our Raman instrument:

BWTEK i-Raman Plus

Model:

BWS465-785H

Excitation:

785 nm

Measurement range:

500–2000 cm⁻¹

Microscope:

BAC102-785E

Objectives:

20× / 50×

Initial acquisition settings will be based on our previously used validated settings.

For example:

- integration time: 10 s

- multiple accumulations

- controlled laser power

- identical acquisition parameters across controls and samples

The actual laser power at the sample should be verified in mW before final quantitative comparisons.

15. LPS Spectral Analysis

The expected LPS bands from literature will be used as search regions, not as proof of detection.

Candidate regions include approximately:

| Region | Interpretation |
| --- | --- |
| ~1131 cm⁻¹ | LPS-associated band reported in literature |
| ~1316 cm⁻¹ | LPS-associated band |
| ~1366 cm⁻¹ | LPS-associated band |
| ~1579 cm⁻¹ | LPS-associated band |
| ~1655 cm⁻¹ | LPS-associated band |

Because our system uses 785 nm, the spectrum must be experimentally checked against the substrate background.

16. Artifact Rejection Rule

This is now a mandatory part of our experimental workflow.

A peak will not be accepted simply because software identifies it.

A candidate LPS feature should satisfy:

Criterion 1 – Reproducibility

It should appear in multiple spectra/spots.

Criterion 2 – Multiple detector pixels

A genuine Raman feature should not exist as a single-pixel detector artifact.

Criterion 3 – Blank comparison

The feature should not simply be a normal Ag/porous-Si background feature.

Criterion 4 – Spectral consistency

The peak position and spectral shape should be reasonably consistent.

Criterion 5 – Concentration response

If possible, increasing LPS concentration should produce a systematic change in the relevant signal.

Only after satisfying these criteria will the signal be treated as a genuine LPS-associated Raman feature.

17. Stage 8 – Concentration Response

If LPS detection is confirmed, move to a concentration series.

Example:

1 nM

↓

10 nM

↓

100 nM

↓

1 µM

↓

10 µM

The purpose is to determine whether the Raman response changes systematically with LPS concentration.

Only after obtaining a genuine concentration-dependent response should we discuss:

- calibration curve

- sensitivity

- LOD

- LOQ

- linear range

18. Stage 9 – Reproducibility

For the selected substrate condition:

Measure:

Multiple spots

For example:

Spot 1 → Spot 2 → Spot 3 → Spot 4 → Spot 5

Then repeat with multiple substrate pieces.

This allows us to determine:

- spot-to-spot variation

- substrate-to-substrate variation

- SERS uniformity

- experimental reproducibility

This is important because SERS can be strongly affected by local hotspots.

19. Stage 10 – Optimize Only After Detection

We will not optimize everything simultaneously.

The optimization hierarchy is:

First

Porous-Si morphology

↓

Second

Ag nanoparticle morphology

↓

Third

R6G SERS performance

↓

Fourth

LPS detection

↓

Fifth

LPS concentration response

↓

Sixth

Measurement/reproducibility optimization

↓

Seventh

Surface localization or functionalization, if necessary

This prevents the experiment from becoming random trial-and-error.

20. If LPS Is Not Detected

A negative result will not immediately mean that the substrate failed.

We will identify where the failure occurred.

Case A

R6G fails.

→ Substrate fabrication/Ag morphology needs investigation.

Case B

R6G works but LPS fails.

→ Investigate LPS adsorption, surface interaction, concentration, droplet localization, and spectral overlap/background.

Case C

LPS appears at one spot only.

→ Investigate hotspot/localization and reproducibility.

Case D

LPS appears reproducibly but weakly.

→ Investigate concentration, integration time, laser power, Ag morphology and surface localization.

Case E

LPS response is reproducible and concentration-dependent.

→ Proceed to quantitative characterization.

21. Important Improvement: Droplet Localization

One of the problems identified from the earlier NAM/LTA experiments was analyte distribution on the surface.

Therefore, if Ag/porous-Si produces a genuine SERS response but poor reproducibility, the next modification can be a localized sensing region.

The concept is:

hydrophilic sensing region

surrounded by

hydrophobic/non-sensing region

so that the droplet preferentially remains over the SERS-active region.

This is based on the localized Ag-nanoparticle-decorated porous-Si approach reported in the literature.

However, this should be introduced after the basic Ag/porous-Si + LPS system is tested, not at the beginning.

22. What We Are NOT Doing Initially

We will not initially introduce:

- antibodies

- aptamers

- boronic-acid functionalization

- Au/Ag bimetallic structures

- complicated microfluidics

- nanolithography

- machine learning

- LOD optimization

- extensive laser-power optimization

These can be future optimization stages.

The first objective is simply:

Can we reproducibly detect LPS using Ag/porous-Si under 785-nm excitation?

23. Role of Machine Learning

Machine learning will be considered only after reliable spectra are obtained.

The sequence will be:

Reliable spectra

↓

Preprocessing

↓

Feature extraction

↓

Concentration-dependent dataset

↓

Classification/regression

↓

ML model

There is no benefit in training a sophisticated model on spectra that contain substrate artifacts or non-reproducible peaks.

24. Final Experimental Decision Tree

n-type Si(100)

↓

Porous-Si fabrication

↓

FESEM characterization

↓

Ag nanoparticle deposition

↓

FESEM + EDS

↓

Ag/porous-Si substrate

↓

R6G SERS validation

↓

┌───┴───┐

│       │

FAIL     PASS

│       │

Optimize  LPS

substrate   ↓

Controls

↓

Ag/porous-Si blank

↓

Ag/porous-Si + LPS

↓

Raman spectra

↓

Artifact rejection

↓

Reproducibility

↓

Concentration series

↓

Concentration response

↓

Quantitative analysis

↓

LOD / LOQ / sensitivity

↓

Further optimization

25. Final Control Matrix

| Sample | Purpose |
| --- | --- |
| Bare Si | Silicon reference |
| Porous-Si | Porous-Si background |
| Ag/porous-Si | SERS substrate blank |
| Ag/porous-Si + R6G | SERS-positive control |
| Ag/porous-Si + LPS | Target detection |
| Ag/porous-Si + different LPS concentrations | Concentration response |

26. Comparison With Our Previous Experiment

| Previous approach | New approach |
| --- | --- |
| Ag/Black-Si | Ag/porous-Si |
| MACE/Black-Si architecture | Controlled porous-Si architecture |
| Ag already integrated with Si structure | Ag deposited after porous-Si formation |
| NAM/LTA attempted | LPS prioritized |
| Strong R6G response | R6G used again as validation |
| Biomarker signal difficult to reproduce | Explicit blank + artifact rejection |
| Repeated optimization risk | Stepwise literature-driven development |
| 785 nm | 785 nm |
| Same Raman instrument | Same Raman instrument |

The new experiment therefore changes the substrate architecture and target biomarker, while keeping the Raman platform controlled.

27. Final Research Logic

The project should be presented as:

Literature evidence → substrate design → fabrication → physical characterization → SERS validation → LPS detection → reproducibility → concentration response → optimization

Not:

Make substrate → try LPS → change parameters until something appears.

The important scientific distinction is that Ag/porous-Si is a literature-supported SERS architecture, while Ag/porous-Si specifically for LPS detection under our 785-nm conditions remains an experimental question.

Therefore, the experiment itself will establish whether the proposed architecture is suitable.

28. Immediate Next Steps

Step 1

Finalize the literature-supported porous-Si fabrication conditions for n-type Si(100), 1–10 Ω·cm.

Step 2

Discuss the fabrication route with Prof. Ajay and confirm the laboratory-approved HF/electrochemical procedure.

Step 3

Fabricate 3 controlled porous-Si conditions.

Step 4

FESEM characterization.

Step 5

Deposit Ag nanoparticles using the selected AgNO₃-based method.

Step 6

FESEM + EDS.

Step 7

R6G SERS validation at 785 nm.

Step 8

Select the most reproducible SERS-active substrate.

Step 9

Run Ag/porous-Si blank.

Step 10

Run LPS concentration screening.

Step 11

Check the reported LPS spectral regions.

Step 12

Apply the artifact-rejection criteria.

Step 13

Repeat measurements across multiple spots/substrates.

Step 14

If genuine LPS detection is obtained, perform concentration-response analysis.

Step 15

Only then optimize sensitivity, localization, functionalization and eventually ML.

Final Experimental Goal

Primary goal:

Develop and validate a reproducible Ag/porous-Si SERS substrate capable of label-free LPS detection using the available 785-nm Raman system.

Secondary goals:

- Establish reproducible porous-Si fabrication.

- Establish reproducible Ag nanoparticle deposition.

- Characterize Ag/porous-Si morphology.

- Validate SERS activity using R6G.

- Determine whether LPS produces reproducible Raman features.

- Determine concentration dependence.

- Quantify reproducibility.

- Optimize the substrate only after genuine LPS detection is demonstrated.

Long-term goal:

Extend the validated platform toward a multi-biomarker SERS sensor for sepsis, including LPS, NAM and LTA, followed by quantitative analysis and machine-learning-assisted classification.

Ag/Porous-Si SERS Substrate for LPS Detection
Target: LPS (E. coli)
Raman: 785 nm

PAGE 1 — SUBSTRATE PREPARATION & VALIDATION

1. Objective

Develop an Ag nanoparticle-decorated porous-Si SERS substrate and evaluate its ability to detect LPS using the available 785-nm Raman system.

Overall workflow:

n-Si → Porous Si → Ag deposition → Characterization → R6G → LPS

2. Silicon Wafer

Available wafer:

- n-type Si

- (100)

- 1–10 Ω·cm

- Single-side polished

Porous Si will be prepared using an electrochemical/anodization method suitable for n-type Si.

Exact HF concentration, current density and etching time will be finalized from literature and the approved laboratory HF SOP.

3. Porous-Si Preparation

Prepare a small set of conditions by varying:

- Etching time

- Current density

- Electrolyte/HF condition

Goal: Obtain reproducible porous structures rather than immediately optimizing all parameters.

Characterization

FESEM → pore morphology and surface structure

Select the most suitable porous-Si condition for Ag deposition.

4. Ag Nanoparticle Deposition

Deposit Ag nanoparticles onto porous Si using an AgNO₃-based immersion/electroless deposition method.

Porous Si + AgNO₃ → Ag nanoparticles/porous Si

Characterize the resulting substrate using:

- FESEM: Ag morphology/distribution

- EDS: confirmation of Ag

5. R6G SERS Validation

Before LPS, test the substrate with R6G.

Purpose: Confirm that Ag/porous-Si is SERS-active at 785 nm.

Check:

- Raman bands

- SNR

- Multiple measurement spots

- Reproducibility

Only substrates showing reproducible R6G enhancement will proceed to LPS testing.

PAGE 2 — LPS DETECTION & VALIDATION

6. LPS Detection

Use Ag/porous-Si for label-free LPS detection.

Initial concentration screening:

1 nM → 10 nM → 100 nM → 1 µM → 10 µM

The final range will be adjusted based on the available LPS stock and literature conditions.

7. Control Samples

| Sample | Purpose |
| --- | --- |
| Bare Si | Si reference |
| Porous-Si | Porous-Si background |
| Ag/porous-Si | Substrate blank |
| Ag/porous-Si + R6G | Positive SERS control |
| Ag/porous-Si + LPS | Target detection |

8. Raman Measurement

Instrument: BWTEK i-Raman Plus
Laser: 785 nm
Range: 500–2000 cm⁻¹
Objective: 20× / 50×
Initial integration: 10 s with multiple accumulations

Keep the acquisition parameters consistent between blank and LPS measurements.

9. LPS Peak Verification

Literature-reported LPS regions will be checked around:

~1131, 1316, 1366, 1579 and 1655 cm⁻¹

These are reference regions only.

A peak will be considered meaningful only if it:

- Appears in multiple spectra/spots.

- Is absent or distinguishable from the Ag/porous-Si blank.

- Is not a single-detector-pixel artifact.

- Has consistent peak position/shape.

- Shows a concentration-dependent response, where possible.

10. Reproducibility

For each important condition:

5 different spots → repeat on independent substrate

Evaluate:

- Spot-to-spot variation

- Substrate-to-substrate variation

- SNR

- Spectral consistency

11. Decision Path

Porous-Si fabrication

↓

FESEM

↓

Ag deposition

↓

FESEM + EDS

↓

R6G validation

↓

LPS + controls

↓

Peak/artifact verification

↓

Reproducibility

↓

LPS concentration response

↓

Sensitivity / LOD / LOQ

12. Important Rule

Can Ag/porous-Si reproducibly detect LPS at 785 nm?

If successful, the next stage will be optimization of Ag morphology, porous-Si structure, concentration, droplet localization and eventually surface functionalization/ML.

Final Goal

Develop a reproducible Ag/porous-Si SERS platform for label-free LPS detection using 785-nm Raman spectroscopy.