# Meeting Discussion Plan — Porous-Si Substrate Proposal

Structure: problem → evidence → proposed experiment → decision criteria

# 1. Start With Current Results

One-slide summary of the current Ag/Black-Si platform:

| Test | Result |
| --- | --- |
| R6G | Successful SERS response |
| NAM | Not reproducibly detected |
| LTA | Apparent ~1095 cm⁻¹ feature later identified as a single-pixel artifact |
| Instrument calibration | Checked using the Si reference peak |

Therefore: the substrate is SERS-active, but biomarker detection is not yet reliable.

“The main question now is whether the limitation is the substrate architecture, analyte–Ag interaction, or analyte localization.”

# 2. Show This Is Not Random Optimization

Key discussion point:

“Instead of continuing trial-and-error on Ag/Black-Si, I want to benchmark a literature-reported Ag/porous-Si architecture.”

Diagram to show:

Existing

Ag / Black-Si

|

| biomarker detection weak

v

------------------

|

v

New literature route

Porous Si

v

Ag nanoparticle deposition

v

Ag / Porous-Si

v

R6G validation

v

LPS detection

The published porous-Si literature gives a defensible reason to investigate this architecture.

# 3. Discuss the Porous-Si Plan

Wafer specification to bring to the discussion: n-type Si(100), 1–10 Ω·cm, single-side polished.

Question to ask:

“Can we fabricate porous Si using our available electrochemical/HF setup, following an appropriate n-type Si literature protocol and our institutional HF SOP?”

Do not commit to a recipe until the literature method is verified to match the actual wafer and available equipment.

# 4. Discuss Ag Deposition

This is likely the most important technical discussion point.

AgNO3 solution

|

v

Ag+

| reduction

v

Ag0

|

v

Ag nanoparticles

|

v

Porous-Si scaffold

“I want to use literature-reported immersion/electroless Ag deposition rather than immediately depending on sputtering.”

Supporting references: Zeiri et al. reported Ag nanoparticle deposition on porous Si from Ag⁺ solution; Kosović et al. investigated Ag-covered porous Si for low-concentration SERS.

# 5. Specific Questions to Bring

| # | Question |
| --- | --- |
| Q1 | Should we proceed with porous Si → Ag deposition as a second substrate architecture? |
| Q2 | Which porous-Si fabrication route should we use for our n-type Si(100), 1–10 Ω·cm wafer? |
| Q3 | Can we fabricate 3–5 porous-Si conditions rather than only one? |
| Q4 | For Ag deposition, should we first reproduce one published AgNO3 immersion condition exactly? |
| Q5 | Can we characterize the porous Si and Ag/porous-Si using FESEM + EDS before biological testing? |
| Q6 | Should LPS remain the first biomarker after R6G validation? |
| Q7 | Should we compare Ag/Black-Si vs Ag/Porous-Si using exactly the same R6G and LPS measurement conditions? |

# 6. Proposed Experimental Decision Tree

Ag/Porous-Si

|

v

FESEM / EDS

|

v

R6G?

/       \

NO         YES

|           |

modify substrate  v

LPS

|

reproducible?

/        \

NO          YES

|            |

investigate       concentration

surface/analyte   series

interaction         |

v

NAM + LTA

# 7. Do Not Discuss LOD Yet

Avoid saying:

“We will achieve nanomolar LPS detection.”

Say instead:

“First we need to establish reproducible detection. LOD and linear range will be determined only after a genuine concentration-dependent response is demonstrated.”

This is the scientifically stronger position.

# 8. Discuss Previous Artifacts

Mention the LTA result directly:

“I initially considered the ~1095 cm⁻¹ feature as a possible LTA signal, but after pixel-level inspection it occupied only one detector pixel, so I excluded it as an artifact.”

This demonstrates that a detection criterion is being applied, rather than forcing a positive result.

Future positive detections must satisfy:

- Expected Raman feature

- Reproducible across spots

- Reproducible across measurements

- Multiple detector pixels

- Distinguishable from blank

- Concentration-dependent behavior where applicable

# 9. What to Leave the Meeting With

Not just “Okay, try porous Si.” Get agreement on five decisions:

| Decision | Need from discussion |
| --- | --- |
| Porous-Si fabrication | Which literature route? |
| Ag deposition | Which published protocol? |
| Characterization | FESEM/EDS available? |
| Positive control | R6G conditions |
| Biomarker | LPS first after validation |

## Closing statement

“My proposal is to stop modifying the existing Ag/Black-Si blindly, reproduce a literature-supported Ag/porous-Si substrate, validate it with R6G, and then perform a controlled Ag/Black-Si versus Ag/porous-Si comparison for LPS. Based on reproducibility, we can decide the next optimization step.”