Document A

Experimental Execution Plan / SOP

AgNO₃ Optimization Series for Bare Ag/Black-Si NAM Detection

____________________________________________________________

Sukesh P (M24IM1007)  |  IIT Jodhpur & AIIMS Jodhpur Joint IDRP  |  13 August 2026

Companion document: Document B — Scientific Rationale and Experimental Decision Log

CONFIRMED — NAM molecular weight corrected: 293.27 g/mol (verified against PubChem CID 5462244 and Sigma-Aldrich product A3007, CAS 10597-89-4), replacing the 275.25 g/mol figure used in earlier documents. The old value was low by exactly one water molecule (18.02 g/mol) — consistent with an anhydrous/dehydration calculation slip. This changes your NAM stock concentration by about 6.5% (see Section 2).

WARNING — Do not begin fabrication from this document until the "Values That Must Be Confirmed" section (next page) has been checked against your actual reagent bottles and instrument. Several quantities below are computed using placeholder assumptions that are explicitly flagged.

# Experiment Summary

| Experiment | Variable | Levels | Constants | Purpose |
| --- | --- | --- | --- | --- |
| Exp. 1 | AgNO₃ concentration | 5, 10, 20, 40, 80 mM (Groups A0-D, see Section 4) | 2-min etch, 8.6 mL HF, 50 mL bath, NAM 1 mg/mL, 5 s / 3 acc. / fixed power | Test whether Ag nanostructure geometry affects NAM detectability, independent of capture chemistry |
| Exp. 2 | (conditional) NAM concentration | 1x / 5x / 10x (3.41 / 17.05 / 34.1 mM) — see Document B decision tree | Best AgNO3 condition from Exp. 1, all else fixed | Distinguish "not enough NAM" from "NAM doesn't stick to bare Ag" — only run if Exp. 1 is negative |
| Exp. 3 | (later, deferred) | Ag deposition cycles / reagent sequence | Best AgNO3 + etch condition | Second-order fabrication refinement — only after Exp. 1-2 are exhausted |
| Exp. 4 | (deferred until MPBA available) | MPBA functionalization | Best bare-Ag condition as substrate | Add covalent capture chemistry — see Document B roadmap |

# Values That Must Be Confirmed Before Starting

Per your instruction, nothing below is invented. These are the specific unresolved inputs, what they affect, and exactly where to get them.

| # | Value | Status / placeholder used here | Affects | Where to obtain it |
| --- | --- | --- | --- | --- |
| 1 | HF stock concentration | Assumed 49% w/w, density 1.15 g/mL — NOT confirmed | Exact molar HF concentration in the bath (Section 2); does not affect AgNO3 masses | Reagent bottle label / certificate of analysis |
| 2 | Exact laser power in mW for power levels "5" and "10" | Unknown — general BWS465-785x class spec found (~30 mW nominal at probe, ~42 mW at laser port) but not confirmed for your exact BTC665N-785H-SYS unit | Whether your two tested power levels are meaningfully different; absolute power reporting | BWSpec software power display, or spec sheet/label on the laser head |
| 3 | Si wafer specifications (resistivity, doping type, orientation, thickness) | Not found in any file/folder — orientation is conventionally (100) for MACE work but not confirmed for your wafers | Etch rate and pore morphology can depend on doping/resistivity; needed for a fully traceable SOP | Wafer box/supplier datasheet |
| 4 | Piranha / RCA cleaning solution concentrations (if used before A1 solvent clean) | Not specified — this SOP assumes only the acetone→IPA→DI solvent clean plus HF oxide-strip, no piranha, per your "today's run sheet" constraint | Starting surface cleanliness/oxide state | Your own protocol notes if piranha was used previously |
| 5 | R6G stock concentration and solvent | 0.1 / 0.01 / 0.001 mM stated in chat; solvent (DI water vs. ethanol) not confirmed | R6G comparability across substrates; ethanol vs water changes drying behavior | Your R6G prep notes |
| 6 | Exact drop volume and pipette precision used previously | 2-3 µL adopted after the coffee-ring issue on 12 Aug; not logged per-file for earlier drops | Reproducibility of deposited mass per spot | Going forward: log this every time (Section 10) |

Items 1-2 do not block starting the AgNO3 series (Section 4) since the AgNO3 masses are independently verified — see Section 2. Items 3-6 should be resolved before treating results as fully publication-traceable.

# 2. Chemical Calculations (Shown From First Principles)

## 2.1  AgNO₃ (verified — does not depend on any assumed value)

Formula: required mass (g) = target molarity (mol/L) × final volume (L) × MW (g/mol). MW of AgNO₃ = 169.87 g/mol.

| Target [AgNO₃] | Fold vs. baseline | Calculation | Mass required in 50 mL |
| --- | --- | --- | --- |
| 5 mM | 0.25x | 0.005 mol/L × 0.050 L × 169.87 g/mol | 0.0425 g |
| 10 mM | 0.5x | 0.010 × 0.050 × 169.87 | 0.0849 g |
| 20 mM | 1x (baseline — as previously fabricated) | 0.020 × 0.050 × 169.87 | 0.1699 g (matches the 0.170 g used on 12 Aug) |
| 40 mM | 2x | 0.040 × 0.050 × 169.87 | 0.3397 g |
| 80 mM | 4x | 0.080 × 0.050 × 169.87 | 0.6795 g |

An intermediate 10 mM point is included here (see Document B Section on series critique) even though it wasn't in the original 4-point proposal — it fills the largest gap in the original series (5→20 mM was a 4x jump while every other step was 2x).

## 2.2  HF (concentration NOT independently verified — placeholder shown)

If the stock is 49% w/w at density 1.15 g/mL: molarity = (0.49 × 1150 g/L) ÷ 20.01 g/mol ≈ 28.2 M.

8.6 mL × 28.2 M ÷ 50 mL final volume ≈ 4.85 M HF in the bath — IF the 49% assumption is correct. This figure is not used for anything decision-critical in this plan (HF volume is held constant across all groups), but should be corrected in your records once Item 1 above is confirmed.

## 2.3  NAM/MurNAc (MW corrected to 293.27 g/mol)

Formula: concentration (mM) = (mg/mL × 1000) ÷ MW (g/mol).

| Prep | Calculation (MW=293.27) | Concentration | Old (wrong, MW=275.25) value |
| --- | --- | --- | --- |
| 1 mg/mL — used 12 Aug | 1000 mg/L ÷ 293.27 g/mol | 3.41 mM | 3.63 mM (6.5% high) |
| 5 mg/mL — proposed 5x | 5000 mg/L ÷ 293.27 g/mol | 17.05 mM | 18.17 mM |
| 10 mg/mL — proposed 10x | 10000 mg/L ÷ 293.27 g/mol | 34.10 mM | 36.33 mM |

WARNING — Any NAM molarity figure in earlier documents (including the previous "Next Experiment Plan") used MW=275.25 g/mol and is approximately 6.5% too high. The mg/mL prep instructions themselves are unaffected (you still weigh the same mass) — only the molarity label was wrong. Re-label existing stock as 3.41 mM, not 3.63 mM.

## 2.4  R6G

MISSING — R6G MW (typically cited as 479.02 g/mol for the chloride salt) was not independently re-verified against your specific reagent bottle in this pass — flagged for completeness, but the three working concentrations (0.1/0.01/0.001 mM) were stated directly by you in mM already, so no conversion is required to use them.

# 2.5  Chemical Preparation Table (Stock / Working / Final-at-Sample)

| Chemical | Stock solution | Working solution | Final conc. at sample | Purpose |
| --- | --- | --- | --- | --- |
| AgNO₃ | Solid, ACS grade (assume ≥99%, purity not confirmed) | Dissolved directly to target: 0.0425-0.6795 g in 50 mL DI (Section 2.1) | N/A — consumed into Ag nanostructure during MACE, not present in final measured sample | MACE catalyst / Ag nanoparticle source |
| HF | Concentrated stock, assumed 49% w/w (UNCONFIRMED, Item 1) | 8.6 mL stock added to AgNO3/DI mixture, topped to 50 mL | N/A — bath is discarded after etch, substrate rinsed | Si etchant in one-step MACE |
| NAM (MurNAc) | 1 mg/mL in DI water = 3.41 mM (working stock, corrected MW) | Same as stock for Exp. 1 (held constant); 5/10 mg/mL for conditional Exp. 2 | Whatever concentration is in the 2-3 µL drop, post-drying (effectively concentrated as solvent evaporates) | Target analyte |
| R6G | 0.1 mM (highest of your 3-point series) | 0.1 / 0.01 / 0.001 mM series, solvent TBC (Item 5) | Same as working — used as deposited | SERS validation / substrate control |
| DI water | N/A (water purification system output) | Solvent for all of the above; also final bath top-up | N/A | Solvent, rinsing |

"Final concentration at sample" is left largely N/A because SERS measurements here are on dried deposits, not solution-phase — the relevant quantity is total mass of analyte delivered to the measured spot (concentration x drop volume), not a solution molarity at the moment of measurement.

# 3. Experimental Groups — Quick Reference

Five groups: the original 4-point proposal (A, B, C, D) plus one inserted point (A2, 10 mM) that closes the uneven gap between A and B — see Document B for the reasoning. All groups share the same etch time, HF volume, NAM prep, and Raman settings; only AgNO3 mass changes.

## GROUP A

| Field | Value |
| --- | --- |
| Experiment ID | EXP-AG05 |
| Substrate ID | EXP-AG05-SUB01 (increment -SUB02, etc. if repeated) |
| AgNO₃ concentration | 5 mM |
| AgNO₃ mass required | 0.0425 g |
| HF volume | 8.6 mL (assumed 49% stock — Item 1) |
| DI water | to final volume of 50 mL total |
| Final bath volume | 50 mL |
| Etch/MACE time | 2 min |
| NAM concentration used | 1 mg/mL = 3.41 mM (held constant — Section 2.3) |
| NAM drop volume | 2-3 µL per spot |
| Raman settings | 785 nm, 5 s integration, 3 accumulations, power level TBD-fixed (Item 2), 400-1800 cm⁻¹ |
| Spots per substrate | ≥3 (blank), ≥3 (R6G), ≥3 (NAM) |

## GROUP A2

| Field | Value |
| --- | --- |
| Experiment ID | EXP-AG10 |
| Substrate ID | EXP-AG10-SUB01 (increment -SUB02, etc. if repeated) |
| AgNO₃ concentration | 10 mM |
| AgNO₃ mass required | 0.0849 g |
| HF volume | 8.6 mL (assumed 49% stock — Item 1) |
| DI water | to final volume of 50 mL total |
| Final bath volume | 50 mL |
| Etch/MACE time | 2 min |
| NAM concentration used | 1 mg/mL = 3.41 mM (held constant — Section 2.3) |
| NAM drop volume | 2-3 µL per spot |
| Raman settings | 785 nm, 5 s integration, 3 accumulations, power level TBD-fixed (Item 2), 400-1800 cm⁻¹ |
| Spots per substrate | ≥3 (blank), ≥3 (R6G), ≥3 (NAM) |

## GROUP B

| Field | Value |
| --- | --- |
| Experiment ID | EXP-AG20 |
| Substrate ID | EXP-AG20-SUB01 (increment -SUB02, etc. if repeated) |
| AgNO₃ concentration | 20 mM (baseline/repeat) |
| AgNO₃ mass required | 0.1699 g |
| HF volume | 8.6 mL (assumed 49% stock — Item 1) |
| DI water | to final volume of 50 mL total |
| Final bath volume | 50 mL |
| Etch/MACE time | 2 min |
| NAM concentration used | 1 mg/mL = 3.41 mM (held constant — Section 2.3) |
| NAM drop volume | 2-3 µL per spot |
| Raman settings | 785 nm, 5 s integration, 3 accumulations, power level TBD-fixed (Item 2), 400-1800 cm⁻¹ |
| Spots per substrate | ≥3 (blank), ≥3 (R6G), ≥3 (NAM) |

## GROUP C

| Field | Value |
| --- | --- |
| Experiment ID | EXP-AG40 |
| Substrate ID | EXP-AG40-SUB01 (increment -SUB02, etc. if repeated) |
| AgNO₃ concentration | 40 mM |
| AgNO₃ mass required | 0.3397 g |
| HF volume | 8.6 mL (assumed 49% stock — Item 1) |
| DI water | to final volume of 50 mL total |
| Final bath volume | 50 mL |
| Etch/MACE time | 2 min |
| NAM concentration used | 1 mg/mL = 3.41 mM (held constant — Section 2.3) |
| NAM drop volume | 2-3 µL per spot |
| Raman settings | 785 nm, 5 s integration, 3 accumulations, power level TBD-fixed (Item 2), 400-1800 cm⁻¹ |
| Spots per substrate | ≥3 (blank), ≥3 (R6G), ≥3 (NAM) |

## GROUP D

| Field | Value |
| --- | --- |
| Experiment ID | EXP-AG80 |
| Substrate ID | EXP-AG80-SUB01 (increment -SUB02, etc. if repeated) |
| AgNO₃ concentration | 80 mM |
| AgNO₃ mass required | 0.6795 g |
| HF volume | 8.6 mL (assumed 49% stock — Item 1) |
| DI water | to final volume of 50 mL total |
| Final bath volume | 50 mL |
| Etch/MACE time | 2 min |
| NAM concentration used | 1 mg/mL = 3.41 mM (held constant — Section 2.3) |
| NAM drop volume | 2-3 µL per spot |
| Raman settings | 785 nm, 5 s integration, 3 accumulations, power level TBD-fixed (Item 2), 400-1800 cm⁻¹ |
| Spots per substrate | ≥3 (blank), ≥3 (R6G), ≥3 (NAM) |

# 5. Silicon Cleaning / Pretreatment (identical for all 5 groups)

Solvent clean (Stage A1). Sequential sonication or rinse in acetone → IPA → DI water. Exact durations not re-confirmed in this pass — use your established protocol from the master SOP (SOP_MACE_NAM_SERS_Bench_Protocol_Aug2026.docx) unless changed.

Native oxide strip (Stage A3). Dilute-HF dip immediately (within ~5 min) before the MACE etch — same protocol as 12 Aug, timing not to be delayed.

Piranha (Stage A2). NOT used in this round, consistent with the 12 Aug "no piranha" run sheet. Note this explicitly in your log so it isn't assumed done later.

MISSING — Si wafer specs (Item 3) — if resistivity/doping type differ between pieces used for different groups, etch rate could differ independent of AgNO3. Confirm all 5 pieces come from the same wafer batch.

# 6. MACE / Ag Deposition Procedure (one-step, identical mechanism across groups)

Dissolve AgNO₃. Weigh the group-specific mass (Section 3 table) into approximately 20 mL DI water in a clean PP/PTFE beaker. Swirl until fully dissolved (AgNO3 is highly soluble; all 5 target masses dissolve readily at room temperature).

Add HF. In a separate PP/PTFE container, measure 8.6 mL concentrated HF. Add the HF to the AgNO3 solution (not the reverse) — this order was used on 12 Aug and is kept constant here.

Top to final volume. Add DI water to bring the total to 50 mL. Swirl gently to mix; avoid splashing.

Immerse the substrate. Immerse the freshly oxide-stripped Si piece immediately. Start the timer.

Etch for 2 minutes. Same across all 5 groups — this is the one previously-validated etch time (Section 1.4 of the previous report), held fixed so AgNO3 is the only variable.

Remove and quench. Remove the substrate at exactly 2:00, rinse immediately and thoroughly with DI water to halt the reaction.

WARNING — Full HF safety protocol applies at every step above: double gloves (HF-rated outer layer), face shield, fume hood, calcium gluconate gel on hand, do not work alone. See master SOP Section 2 for complete detail.

# 7. Washing, Drying, and Storage

Wash: thorough DI water rinse immediately post-etch (above), then a second brief DI rinse before drying.

Dry: dry nitrogen blow-dry if available, otherwise air-dry in a covered, particle-free container. Do not wipe the surface.

Storage: IPA immersion if not measured same-day (consistent with 12 Aug protocol); label the vial with the Experiment ID immediately, before setting it down.

# 8. NAM Preparation and Deposition

## 8.1  Stock preparation

1 mg NAM per 1 mL DI water = 3.41 mM (Section 2.3, corrected MW). Weigh on an analytical balance; record actual mass and volume used (not just the target) in the log — see Section 11.

## 8.2  Deposition procedure (per spot)

Confine the drop. Given the coffee-ring/spreading issue observed on 12 Aug (black-Si is superhydrophilic), use a hydrophobic barrier (wax/PAP pen ring) around each target spot before dropping, OR keep to 2-3 µL and accept a wider raster search area if no barrier is available.

Deposit 2-3 µL of the 1 mg/mL (3.41 mM) NAM stock at the marked spot.

Air-dry fully, undisturbed. Do not blow or heat-dry (worsens ring formation). Record actual dry time observed.

Repeat at ≥3 separate spots on the same substrate, each spaced far enough apart to avoid cross-contamination.

MISSING — Exact dry time was not controlled/logged on 12 Aug. Going forward, time from deposition to a visually dry spot and record it — this is a real experimental variable (evaporation rate affects deposit morphology/ring formation).

# 9. Raman Measurement Procedure

Order per substrate: blank (bare, post-etch) → R6G spot-check → NAM (≥3 spots). Blank is always taken first, same session, same settings as the samples that follow it on that substrate.

| Setting | Value | Notes |
| --- | --- | --- |
| Laser wavelength | 785 nm (784.92 nm actual) | Fixed — do not switch mid-series |
| Integration time | 5 s | Matches 12 Aug main dataset |
| Accumulations | 3 | Matches 12 Aug main dataset |
| Laser power level | Pick ONE of {5,10} and use for every group | See Item 2 — exact mW unconfirmed, but internal consistency across groups is what matters most here |
| Spectral range | 400-1800 cm⁻¹ | Covers all target R6G and NAM peaks |
| Spots per sample type | ≥3 | Blank, R6G, NAM each |

# 10. Sample / File Naming Convention

Format: EXP-NAM-AG{concentration}-{SAMPLETYPE}-S{spot#}

| Example | Meaning |
| --- | --- |
| EXP-NAM-AG05-BLANK-S01 | Group A (5 mM AgNO3), blank spectrum, spot 1 |
| EXP-NAM-AG05-R6G-S01 | Group A, R6G, spot 1 |
| EXP-NAM-AG05-NAM-S01 | Group A, NAM, spot 1 |
| EXP-NAM-AG10-NAM-S02 | Group A2 (10 mM), NAM, spot 2 |
| EXP-NAM-AG20-BLANK-S01 | Group B (20 mM baseline), blank, spot 1 |
| EXP-NAM-AG80-R6G-S03 | Group D (80 mM), R6G, spot 3 |

Use this as the actual instrument save-name where possible, or as a mapping column in your log sheet if the instrument software enforces its own naming (as with today's SP_NN.csv sequential names) — this is exactly the gap that made classifying 12 Aug's 177 files by folder-name-inference necessary rather than direct.

# 11. Recommended Logging Spreadsheet

One row per spectrum. Columns:

Column

Date

Experiment ID

Substrate ID

AgNO3 concentration (mM)

AgNO3 mass (g)

HF concentration (assumed/confirmed)

HF volume (mL)

Final bath volume (mL)

Etch time (min)

Si batch/wafer ID

NAM stock (mg/mL)

NAM concentration (mM)

NAM drop volume (µL)

R6G concentration (mM)

Laser power level

Laser power (mW, if known)

Integration time (s)

Accumulations

Spot #

Sample type (Blank/R6G/NAM)

File name

Peak 1 pos/height/SNR

Peak 2 pos/height/SNR

Peak 3 pos/height/SNR

Notes

A single running spreadsheet across all groups, filled in live during measurement, would have prevented the file-classification work needed to analyze 12 Aug's data after the fact.

# 12. Data Analysis Plan

## 12.1  Processing steps

Baseline correction. Asymmetric least-squares or similar, consistent with the method already validated in your NAM manuscript (λ=10⁵, p=0.001, per that document's Section 2.5) — applied identically to every spectrum so groups stay comparable.

Smoothing (optional). Savitzky-Golay only if raw spectra are visibly noisy; apply identically across all groups if used at all, never selectively.

Normalization. Do NOT normalize away intensity differences between AgNO3 groups — raw (dark-subtracted) intensity is the signal you're trying to compare. Normalize only within a single spectrum if comparing peak ratios.

## 12.2  Metrics

SNR. Peak height above a local flanking baseline, divided by noise std from a peak-free region (e.g. 2400-2800 cm⁻¹) — same method used to analyze the 12 Aug dataset, for direct comparability.

Peak height and peak area. Report both; height for quick SNR screening, area for more robust comparison when peaks are broad or overlapping.

Peak position. Compare to your own manuscript reference table and to standard R6G positions; report actual found position, not just target.

Reproducibility. Fraction of spots (within a substrate) and fraction of independent substrates (across repeats) where a given peak clears the SNR threshold.

Coefficient of variation (CV). Std/mean of peak height across spots on one substrate (spot-to-spot) and across repeat substrates of the same group (substrate-to-substrate) — report both, don't conflate them.

## 12.3  Detection criteria

| Category | Criteria |
| --- | --- |
| Detected | ≥2 of the primary NAM bands (930, 871 cm⁻¹) at SNR ≥ 3, reproducible in ≥2 of ≥3 spots on the same substrate, AND consistent position (±5 cm⁻¹) across those spots |
| Possibly detected | 1 primary band at SNR ≥ 3 in ≥1 spot, OR both primary bands at SNR 2-3 (borderline) — flag for repeat measurement, don't report as a positive result |
| Not detected | No primary band reaches SNR ≥ 3 in any spot, or only isolated single-spot hits with no cross-spot repeat (this was the 12 Aug outcome across all conditions tested) |

WARNING — A single peak in a single spot is explicitly NOT sufficient for "detected," per your own instruction — this matches how the 12 Aug isolated SNR≈3 hits (930 cm⁻1 on 10m, 1023 cm⁻1 on 2m) were correctly treated as inconclusive rather than positive.

MISSING — NAM diagnostic peaks (930, 871 cm⁻1 as primary; 541, 1023, 1347, 1394 cm⁻1 as secondary) are taken directly from your own manuscript's experimental reference table — not invented. No published SERS-specific (as opposed to powder Raman) NAM peak list was found in the literature search for this or the previous report, so these positions are the best available reference, but their behavior under SERS (vs. powder Raman) enhancement has not been independently confirmed.

# 13. Blanks and Replicates — Definitions and Structure

## 13.1  Definitions

Technical replicate: the same spot, measured twice (e.g., 2 spectra back-to-back without moving the stage). Tells you instrument/measurement noise only.

Spot-to-spot variation: different spots on the same substrate. Tells you within-substrate nanostructure uniformity.

Independent/substrate replicate: a separate substrate fabricated under nominally identical conditions (e.g., a second 20 mM piece). Tells you fabrication reproducibility — this is what's missing for the 2-min/20 mM condition per the previous report's Section 5.

## 13.2  What to average, and what not to

Average technical replicates at the same spot freely — they represent the same physical measurement.

Do NOT average spot-to-spot spectra into a single number before computing reproducibility — first evaluate each spot individually against the detection criteria (Section 12.3), THEN summarize how many spots passed.

Do NOT average across AgNO3 groups — they are different experimental conditions by design.

Averaging across independent substrates of the SAME condition is appropriate only after confirming they behave consistently (similar peak positions/heights) — report the substrate-to-substrate CV alongside any averaged spectrum.

## 13.3  Required minimum per substrate

| Sample type | Min. spots | Min. spectra/spot | Purpose |
| --- | --- | --- | --- |
| Blank | 3 | 1-2 | Background/substrate-only reference, same-session, same settings as R6G/NAM below |
| R6G | 3 (spot-check) or full 3-conc. series on winner | 1-2 | Go/no-go SERS-activity gate (Section 9 of previous report) |
| NAM | ≥3 | 1-2 | Primary measurement — detection criteria applied per spot (Section 12.3) |

# 14. Safety Checkpoints

WARNING — Every group involves concentrated HF (oxide strip + MACE bath). Full protocol applies at every session: double gloves with HF-rated outer layer, face shield, fume hood, calcium gluconate gel on hand, never work alone, no working alone at any stage from Section 5 through Section 7.

Confirm calcium gluconate gel is present and in date before starting any group.

Confirm a second person is aware you are running an HF session.

Prepare all 5 AgNO3/HF baths in labeled, separate PP/PTFE containers — never reuse a container between groups without a full acid-safe cleaning cycle.

Waste segregation: acid stream vs. silver/heavy-metal stream, per master SOP.

# 15. Decision Criteria for Selecting the Best Substrate (Recap)

Step 1 — R6G gate. Discard any group whose R6G spot-check doesn't clear SNR ≥ 10 at 1509 cm⁻¹.

Step 2 — R6G reproducibility. Among groups that pass Step 1, prefer lowest spot-to-spot CV.

Step 3 — NAM peak count. Rank remaining groups by Section 12.3 "Detected"/"Possibly detected" outcome.

Step 4 — Magnitude as tiebreaker only. Higher SNR breaks ties between two groups that both show genuine, reproducible NAM signal.

Full reasoning behind these criteria, and what each possible outcome implies scientifically, is in Document B.