Today's Run Sheet

Bare-Silver MACE Substrate + Free NAM Deposition (No Piranha, No Boronic Acid)

____________________________________________________________

Prepared for:  Sukesh P (M24IM1007)  |  Date: 8 August 2026

This is a trimmed run sheet derived from the master SOP (SOP_MACE_NAM_SERS_Bench_Protocol_Aug2026.docx). Two steps are deliberately skipped today: Stage A2 (piranha clean) and Stage C0 (MPBA boronic-acid functionalization). Everything else is unchanged.

⚠ This run still uses concentrated HF (Stage A3 and Stage B). Full HF safety requirements apply: double gloves (HF-rated outer layer), face shield, fume hood, calcium gluconate gel on hand, do not work alone. See the master SOP Section 2 for complete detail — this sheet assumes you have already read it.

## What today's run actually tests

With no capture chemistry applied, this run reproduces the project's known bare-Ag condition — per the companion research, this is expected to show little or no NAM signal, and that is a valid, useful result: it is one of the two required reference conditions (the other being R6G on the same batch) that every future functionalized run must be compared against. Treat today as establishing/reconfirming that baseline, not as a failed attempt if NAM shows nothing.

# Materials Needed Today

| Reagent | Grade/Concentration | Quantity |
| --- | --- | --- |
| Acetone | Semiconductor/electronic grade | ~50 mL |
| Isopropyl alcohol (IPA) | Semiconductor/electronic grade | ~50 mL |
| DI water (18.2 MOhm) | - | ~150 mL total |
| Hydrofluoric acid (HF) | 48-49% aqueous, concentrated stock | ~12.5 mL total (4.1 mL oxide-strip + 8.3 mL MACE bath) |
| Silver nitrate (AgNO3) | ACS reagent grade, solid | 0.17 g |
| N-acetylmuramic acid (NAM) | Your existing project stock | ~14 mg or equivalent volume of existing stock solution |
| Nitrogen gas (N2) | Dry, for blow-drying | as needed |
| Calcium gluconate gel (2.5%) | First-aid, HF-specific | on hand, not consumed |

Not needed today: H2SO4, H2O2 (piranha, skipped), MPBA, ethanol (boronic-acid functionalization, skipped).

# Stage A1 — Solvent Clean

| Step | Reagent/Volume | Time | Notes |
| --- | --- | --- | --- |
| A1.1 | Acetone, ~50 mL, fully submerge substrate | 5 min (ultrasonicate if available) | Removes organic residues, dust, fingerprints |
| A1.2 | IPA, ~50 mL, fresh beaker | 5 min (ultrasonicate if available) | Displaces acetone residue |
| A1.3 | DI water rinse | 3 changes, ~30 sec swirl each | Keep substrate wet going into A3 |

# Stage A3 — Native Oxide Strip (skip A2 piranha, go straight here)

Target: ~10% HF, 20 mL total.

| Component | Amount | Calculation |
| --- | --- | --- |
| 48-49% HF stock (~28.9 M) | 4.1 mL | (10% x 20mL)/49% = 4.08 mL -> 4.1 mL |
| DI water | 15.9 mL | 20 mL total - 4.1 mL HF |
| Total dip volume | 20 mL | PP/PTFE dish, fully submerge the chip |

Dip 30-60 seconds.

Brief DI water rinse (a few seconds only).

N2 dry.

PROCEED DIRECTLY to Stage B, ideally within 5 minutes — have the MACE bath already prepared and waiting before you start this dip, since native oxide regrows on bare Si within minutes of air exposure.

# Stage B — MACE Etch (prepare BEFORE you start the A3 dip)

Target: 4.8 M HF, 20 mM AgNO3, 50 mL total.

| Component | Amount | Calculation |
| --- | --- | --- |
| DI water (dissolve AgNO3 in this first) | ~20 mL | Working volume |
| Silver nitrate (AgNO3), solid | 0.17 g | 0.020 mol/L x 0.050 L x 169.87 g/mol = 0.1699 g |
| 48-49% HF stock (~28.9 M) | 8.3 mL | (4.8M x 50mL)/28.9M = 8.30 mL |
| DI water, top-up | ~21.7 mL | To reach 50 mL total |
| TOTAL BATH VOLUME | 50 mL | 4.8 M HF / 20 mM AgNO3 |

Mixing order: dissolve AgNO3 in the 20 mL DI water first (protect from bright light). In the fume hood, add the 8.3 mL HF to this solution (acid to solution, not reverse). Top up to 50 mL. Use immediately.

| Parameter | Value |
| --- | --- |
| Temperature | Room temperature (~22-25C) |
| Immersion time | 10 minutes (start here; 5-10 min if biasing toward denser/smaller Ag spacing) |
| Agitation | None (static immersion) |

Remove with PTFE-tipped tweezers.

DI water rinse: 3 changes, ~30 sec each.

N2 dry (directional stream).

Inspect: surface should look visibly darker/matte ("black silicon") vs. the shiny starting wafer. Note the actual appearance in your batch log.

# Stage C — NAM Deposition on Bare-Ag Substrate (no functionalization today)

## C1. NAM Stock Solution

| Component | Amount | Calculation |
| --- | --- | --- |
| NAM | ~14 mg | 5 mM in 10 mL: 0.005 mol/L x 0.010L x 275.25 g/mol = 13.76 mg. Verify MW against your reagent's certificate of analysis. |
| DI water | 10 mL | Prepare fresh |

## C2-C5. Deposit, Incubate, Wash, Dry

| Step | Action |
| --- | --- |
| C2 | Drop-cast 10 uL of NAM stock onto the bare-Ag substrate surface, centrally on the SERS-active area |
| C3 | Incubate 30 min at room temperature, covered (petri dish) |
| C4 | Optional: split into washed (5-10 sec DI dip) vs. unwashed for comparison if you have two substrate pieces available |
| C5 | N2 dry |

# Stage D — Raman/SERS Measurement

| Parameter | Starting Value |
| --- | --- |
| Laser wavelength | 785 nm |
| Laser power | Lowest usable setting first; increase only if needed, watch for photodamage |
| Integration time | 10 sec x 3 accumulations, adjust for signal-to-noise |
| Acquisition mode | Multi-point grid (10x10 minimum), not a single spectrum |
| Spectral range | 400-1800 cm-1 (include Si 520-521 cm-1 as internal reference) |

## Run alongside this NAM measurement, same session, same batch

Blank: bare-Ag substrate + DI water only, no NAM.

R6G positive control on a substrate from this same fabrication batch, to confirm this batch's SERS activity is intact regardless of the NAM result.

# Batch Record Log — Today

| Field | Value |
| --- | --- |
| Date / Operator |  |
| Substrate ID(s) |  |
| HF stock bottle lot # / opened date |  |
| AgNO3 lot # |  |
| Oxide-strip HF % actually used |  |
| MACE bath: actual HF volume / AgNO3 mass / final volume |  |
| MACE immersion time actual |  |
| Visual result after etch (color/texture) |  |
| NAM concentration actual / volume dropped |  |
| Incubation time actual / washed or unwashed |  |
| Raman: power / integration time / accumulations actual |  |
| Result summary (signal Y/N, R6G control passed Y/N) |  |
| Notes / deviations |  |

# Next Steps

This run establishes/reconfirms the bare-Ag baseline. Once you have MPBA (or a substitute like cysteamine) on hand, repeat Stage A-B identically, add the functionalization step (Stage C0 from the master SOP) before Stage C1, and compare the resulting spectra directly against today's bare-Ag result and the R6G control from the same batch. Log today's batch ID somewhere you can reference it — it's the reference condition every future functionalized run needs to beat.