# Capture and Enhancement Strategies for LPS Detection

Reagent now in hand: Sigma-Aldrich L2630-10MG

Project: SERS nanobiosensor for rapid bacterial identification in sepsis

Prepared: August 2026

# 1. The reagent, and why it matters for strategy

| Property | Value |
| --- | --- |
| Source | Escherichia coli O111:B4 |
| Supplier / catalogue | Sigma-Aldrich, L2630-10MG |
| CAS / EC | 93572-42-0 / 297-473-0 |
| Purification | Phenol extraction (Westphal method) |
| Protein impurity | ≤3% |
| Form | Lyophilised powder, water-soluble |
| Storage | 2–8 °C |

Two things about this specific reagent shape everything below.

First, phenol extraction preserves the O-antigen. Unlike TCA-extracted or deep-rough preparations, Westphal phenol extraction yields predominantly smooth LPS — intact Lipid A, core oligosaccharide, and the full O111 O-antigen repeat. This matters directly for capture chemistry: any strategy that targets the core sugars (boronic acid) has to reach past the O-antigen to get there, while any strategy that targets Lipid A's phosphates (cationic capture, antibody) is targeting a group that sits at the base of the molecule, also somewhat shielded by the polysaccharide above it.

Second, this is functionally the same reagent used in the closest published precedent. Rusciano et al. (2023) — the most directly comparable SERS-LPS study, and already the anchor reference in this project's prior literature review — used Sigma-Aldrich LPS from E. coli O111:B4 (catalogue L6529, a different purification/purity grade of the same serotype). This project's L2630 is close enough in identity that their reported figures function as a real benchmark, not just a qualitative comparison: same organism, same serotype, same supplier family. This is worth stating early because it changes the value of the very first experiment — a bare-substrate LPS measurement here is directly comparable to their Cmin ≈ 3 ng/mL result, not just “in the right ballpark.”

# 2. LPS's chemical handles — a genuinely different situation from NAM

The NAM capture document (previous strategy note) treated NAM as a hard case: small, non-aromatic, no chromophore, weak intrinsic affinity for bare silver. LPS is a different molecule in almost every relevant respect.

| Feature | Location | Relevance to capture |
| --- | --- | --- |
| Phosphate groups (×2) | Lipid A, 1 and 4′ positions | Strongly anionic at pH 7; genuine electrostatic handle |
| Acyl chains (4–6, hydrophobic) | Lipid A | Amphiphilic — can physisorb to a bare metal surface via hydrophobic contact, not just charge |
| KDO carboxylate + vicinal diol | Core, innermost sugar | A genuine cis-diol — unlike NAM, a real boronic-acid target |
| Heptose diols | Core | Additional diol sites, same accessibility caveat |
| Core phosphates | Core oligosaccharide | Further anionic character, reinforcing the electrostatic case |
| O-antigen repeat units | Distal, O111-specific | Hydrophilic, serotype-defining; likely shields the core and Lipid A in smooth LPS |

The practical consequence: LPS is amphiphilic and multiply anionic, with a combination of hydrophobic and electrostatic character that gives it real intrinsic affinity for a bare metal surface. This is precisely the property NAM lacked. It is also large and structurally heterogeneous (batch-to-batch and even molecule-to-molecule micellar aggregation state varies), which cuts the other way — spectra are broader and less easily assigned than a small molecule's.

# 3. Capture strategies, ranked

## 3.1 Direct adsorption — no capture chemistry at all

Try this first, and expect it to actually work. This is the single biggest strategic difference from NAM.

| Method | Drop-cast LPS solution onto the existing substrate, dry, measure the 2850–2950 cm⁻¹ region (Lipid A acyl C–H stretches) |
| --- | --- |
| Precedent | Rusciano et al. (2023) measured bare, unfunctionalised silver substrates dosed directly with E. coli O111:B4 LPS and extrapolated a Cmin of ≈3 ng/mL from the 2900 cm⁻¹ band — before any antibody was added. Verde et al. (2021, Front. Immunol.) independently demonstrated label-free LPS SERS on bare 50 nm AuNPs. |
| Mechanism | Acyl-chain physisorption plus electrostatic attraction of the phosphate groups to the metal — LPS does not need a designed anchor to reach the surface |
| Effort | Trivial — one afternoon |
| Likelihood | High, on existing precedent with the same serotype |

This should be the very first LPS experiment run on the current substrate. If it reproduces even roughly what Rusciano's bare-substrate measurement showed, that is a strong, fast signal that the existing fabrication is fine for LPS — resolving, for this biomarker at least, the substrate-vs-chemistry ambiguity that has been the project's central open question.

## 3.2 Cationic capture layer — exploiting the net negative charge

LPS is anionic at physiological pH (Lipid A phosphates plus KDO/core carboxylates and phosphates). A cationic surface concentrates it directly, the same logic used for NAM's carboxylate but with a much stronger charge handle here.

| Reagent | Support | Notes |
| --- | --- | --- |
| Cysteamine (HS–CH₂CH₂–NH₂) | Ag/Au via thiol | Simple, routine overnight self-assembly |
| Chitosan | either, electrostatic anchoring | Precedented for LPS specifically — Chi-AgNPs used for electrochemical LPS biosensing (Kim et al., Micromachines 2020); multivalent binding |
| Polymyxin B | Ag/Au, adsorbed or thiolated | Not a generic cationic layer — a genuine Lipid A-binding ligand. Cyclic cationic lipopeptide, basis of clinical endotoxin-neutralisation assays; real selectivity for LPS over other anionic serum species |

Recommendation within this tier: skip straight to polymyxin B if resources allow. Cysteamine/chitosan mainly answer “does concentrating LPS at the surface help at all,” a question direct adsorption (§3.1) may already answer on its own.

## 3.3 Boronic acid — the strategy already in place, now aimed at its real target

The NAM document's verdict on boronic acid was: “the right choice for a different target.” This reagent is that target.

| Site | KDO carboxylate + vicinal diol; heptose diols in the core |
| --- | --- |
| Bond formed | Boronate ester, reversible |
| Precedent | A CRISPR/Cas12a + boronic-ester + LPS-aptamer dual-recognition assay (Anal. Chem. 2022) confirms boronic-acid–LPS binding is real and usable in an assay context |
| Caveat specific to this reagent | Because L2630 is phenol-extracted smooth LPS, the O-antigen may sterically shield the core diols from a surface-bound boronic acid ligand — a different failure mode from NAM's (steric vs chemical) but the same practical consequence |

Recommended test, directly analogous to the NAM binding check: compare 4-MPBA reporter-band response (1072/1585 cm⁻¹) on exposure to this LPS versus a simple diol (fructose) at matched concentration, and — if resources allow — versus a rough or deep-rough LPS / free Lipid A standard, where the core is not O-antigen-shielded. A large response to fructose but a small one to smooth LPS, recovered on the rough form, would confirm shielding rather than a fundamentally unreactive core.

This is also the step that most directly reuses existing project infrastructure — the same 4-MPBA monolayer already being developed for NAM.

## 3.4 Anti-Lipid A antibody — highest selectivity, direct benchmark available

| Reagent | Commercial polyclonal anti-Lipid A / anti-LPS antibody |
| --- | --- |
| Mechanism | Not direct LPS detection. The antibody itself is the Raman reporter; LPS binding perturbs the antibody's own SERS spectrum (frequency shift, band splitting near 1660 cm⁻¹, blue-shift of the 2900 cm⁻¹ envelope) |
| Precedent | Rusciano et al. (2023), same serotype: LOD 12 ng/mL, LOQ 41 ng/mL, established via SNR-based extrapolation on real (not extrapolated) binding data |
| Selectivity | High — the antibody-antigen step does the discrimination, not the substrate |
| Cost / effort | Antibody cost; two-stage functionalisation (Ab coating, then blocking solution); readout requires multivariate analysis (PCA), since changes are broad and distributed |

This is the most rigorously benchmarkable option in this whole document. Because the organism and serotype match Rusciano's study, a result here is a direct head-to-head comparison, not a “similar system” comparison — a genuinely rare position to be in.

## 3.5 Molecularly imprinted polymers (MIP)

A polymer cast around LPS (or Lipid A) as template, then the template removed, leaving shape- and charge-complementary cavities.

| Precedent | Özsoylu et al. (2026, Chem. Eng. J.) — LPS-templated biomimetic MIP surfaces for high-affinity bacterial capture; a related 2024 Anal. Chem. MIP targets bacterial outer-membrane vesicles |
| --- | --- |
| Selectivity | Potentially high, and — unlike an antibody — stable at room temperature, relevant for a point-of-care device |
| Effort | High; polymer optimisation is a project in itself |
| Timescale | Months |

Actively published (2023–2026), so this is a credible, not speculative, future direction — but not appropriate for the current timeframe.

## 3.6 Linear polymer affinity agents + machine learning (2025)

A newer category worth flagging explicitly. A 2025 study (ACS Appl. Mater. Interfaces) used broad-affinity linear polymer capture agents (not antibody, not a single-target small molecule) immobilised on a metal-film-over-nanosphere substrate, combined with machine learning classification, to detect and differentiate LPS from multiple foodborne pathogens by spectral fingerprint rather than by a single diagnostic band.

| Advantage | Captures LPS broadly (serotype-agnostic), then relies on ML to distinguish sources — sidesteps the need for a serotype-specific binder |
| --- | --- |
| Relevance here | Directly applicable to this project's stated goal of Gram-class (and potentially organism-level) discrimination from a single sensing channel |
| Effort | Moderate — depends on sourcing/synthesising the affinity polymer; ML pipeline is a natural extension of work already done for NAM/R6G peak-matching |
| Maturity | New (2025); worth tracking rather than committing to immediately |

## 3.7 Aptamers

SELEX-selected oligonucleotides against LPS exist in the literature (used directly in the CRISPR/Cas12a boronic-ester assay cited in §3.3) and offer high selectivity without an antibody's cold-chain fragility. As with the NAM document's assessment, a full SELEX campaign is 6–12 months and not appropriate now — but a commercially available anti-LPS aptamer, if one can be sourced off the shelf, would skip that timeline entirely and is worth a quick supplier check before ruling this out.

# 4. Signal strategies

## 4.1 Direct detection

LPS's own bands are, unlike NAM's, reasonably well characterised in the SERS literature even if broad: Lipid A acyl C–H stretching (2850–2950 cm⁻¹, diagnostic and used directly by Rusciano for the bare-substrate measurement), amide/C=O modes near 1650–1660 cm⁻¹, C–N stretching near 1250 cm⁻¹, and core-sugar ring modes in the 800–1150 cm⁻¹ fingerprint region. Expect broad, overlapping bands rather than the sharp, well-separated peaks seen for NAM — this is a large, structurally heterogeneous molecule, and multi-Gaussian deconvolution (as Rusciano used for the 2900 cm⁻¹ envelope) or full multivariate analysis (PCA, or ML per §3.6) is the realistic path to a quantitative readout, not single-peak intensity.

## 4.2 Indirect / reporter-perturbation assay

The antibody strategy (§3.4) is a specific case of this: a strong Raman reporter's own spectrum shifts or splits when LPS binds nearby, and the change — not an LPS band — carries the concentration information. This generalises beyond antibodies: a polymyxin B–dye conjugate, following the logic of clinical endotoxin-neutralisation assays, could serve the same reporter role at lower cost than a full antibody.

## 4.3 Machine-learning-assisted classification

Increasingly the standard approach for LPS/endotoxin SERS specifically — Yang et al. (2022, Nanoscale) differentiated bacterial endotoxins by SERS plus ML; “DeepRaman” (2025) extends this; the linear-polymer-affinity study (§3.6) pairs broad capture with ML discrimination. Given that this project already has DFT-grounded peak assignments and a working Python/computational pipeline from the NAM work, extending toward classification (rather than single-band quantification) is a natural and comparatively low-cost next step once real LPS spectra exist.

# 5. Recommended sequence

Ordered by information gained per unit effort, and updated for the fact that this reagent is a direct match to the closest published precedent.

| Priority | Action | Effort | Answers |
| --- | --- | --- | --- |
| 1 | Drop-cast LPS on bare existing substrate; measure 2850–2950 cm⁻¹ | 1 day | Does the existing substrate reproduce Rusciano's bare-substrate Cmin (~3 ng/mL) for the same serotype? |
| 2 | Same on a commercial SERS substrate | 1 day + purchase | Separates fabrication issues from LPS-specific issues (same logic as the NAM plan) |
| 3 | Polymyxin B capture layer | 1 week | Does a genuine Lipid A ligand outperform bare adsorption, particularly in a serum-like background? |
| 4 | 4-MPBA boronic acid monolayer (existing chemistry) | 1–2 weeks | Does the core diol bind, or is it O-antigen-shielded — test against fructose and, if available, a rough-LPS control |
| 5 | Anti-Lipid A antibody, frequency-shift readout | 2–3 weeks | Direct, same-serotype benchmark against Rusciano's 12/41 ng/mL LOD/LOQ |
| 6 | Cysteamine/chitosan generic cationic layer | 3 days | Lower priority than polymyxin B; mainly useful if polymyxin B is unavailable |
| 7 | Linear polymer affinity agent + ML classification | Weeks–months | Multiplex/serotype-agnostic capture — aligns with the project's Gram-class discrimination goal |
| 8 | MIP | Months | Long-term selectivity, room-temperature-stable alternative to antibody |
| 9 | Aptamer (SELEX campaign) | 6–12 months | Only if no off-the-shelf aptamer can be sourced |

Steps 1 and 2 together cost two days and, unusually for this project, compare directly against a published number rather than an unknown. They should be run before anything else involving this reagent.

# 6. What I would tell the professor

Three points:

This reagent is a near-exact match to the strongest published precedent this project has. Rusciano et al. (2023) used the same organism and serotype (E. coli O111:B4) from the same supplier family. Every experiment run with this LPS can be benchmarked against a real, published LOD/LOQ (12/41 ng/mL, or Cmin ≈3 ng/mL for bare-substrate detection) rather than compared only qualitatively to “similar” work.

LPS is intrinsically far more SERS-favourable than NAM. It is amphiphilic and multiply anionic — properties that give it real affinity for a bare metal surface without any capture chemistry — where NAM had essentially none. The first experiment should be the cheapest one: direct adsorption on the existing substrate.

Boronic acid, already the project's working chemistry, is aimed at the wrong analyte if used for free NAM, but is aimed at the right one here. LPS's core KDO and heptose residues carry genuine, unblocked cis-diols. The open question for this reagent specifically is not whether the chemistry exists, but whether the intact O111 O-antigen (a consequence of choosing the phenol-extraction / smooth-LPS product) sterically shields those diols — a one-week experiment, not a redesign.

# References

1. Rusciano, G.; Capaccio, A.; Sasso, A.; Capo, A.; Almuzara, C.M.; Staiano, M.; D’Auria, S.; Varriale, A. “A Surface-Enhanced Raman Spectroscopy-Based Biosensor for the Detection of Biological Macromolecules: The Case of the Lipopolysaccharide Endotoxin Molecules.” Int. J. Mol. Sci. 24(15):12099 (2023). DOI:10.3390/ijms241512099. [Uses E. coli O111:B4 LPS, Sigma-Aldrich L6529 — same serotype/supplier family as this project's L2630.]

2. Verde, A.; Mangini, M.; Managò, S.; Tramontano, C.; Rea, I.; Boraschi, D.; Italiani, P.; De Luca, A.C. “SERS sensing of bacterial endotoxin on gold nanoparticles.” Front. Immunol. 12:758410 (2021).

3. Yang, D.; Xu, S.; Haverstick, J.; Ibtehaz, N.; Muszyński, A.; Chen, X.; Chowdhury, R.; Zughaier, S.M.; Zhao, Y. “Differentiation and classification of bacterial endotoxins based on surface enhanced Raman scattering and advanced machine learning.” Nanoscale 14(24):8806–8817 (2022). DOI:10.1039/d2nr01277d.

4. “DeepRaman: Implementing SERS with cutting-edge machine learning for differentiation/classification of bacterial endotoxins.” (2025).

5. CRISPR/Cas12a + boronic ester + LPS aptamer dual-recognition assay. Anal. Chem. (2022). PubMed 36040369.

6. Kim, H. et al. “Chitosan Stabilized Silver Nanoparticles for the Electrochemical Detection of Lipopolysaccharide: A Facile Biosensing Approach for Gram-Negative Bacteria.” Micromachines 11(4):413 (2020). PMC7231338.

7. Özsoylu, D.; Börmann-El Kholy, E.; Wagner, P.; Schöning, M.J. “Lipopolysaccharide-templated biomimetic MIP surfaces for high-affinity bacterial capture.” Chem. Eng. J. (2026).

8. “Lipopolysaccharide Imprinted Polymers for Specific Recognition of Bacterial Outer Membrane Vesicles.” Anal. Chem. (2024). DOI:10.1021/acs.analchem.4c05288.

9. “A Machine Learning-Enabled SERS Sensor: Multiplex Detection of Lipopolysaccharides from Foodborne Pathogenic Bacteria.” ACS Appl. Mater. Interfaces (2025). DOI:10.1021/acsami.5c08361.

10. Sigma-Aldrich product page, Lipopolysaccharides from E. coli O111:B4, L2630 (CAS 93572-42-0, EC 297-473-0).

Citation details to be independently verified against the primary sources before use in a formal report, consistent with the practice followed for the NAM capture-strategy document.